1- The amount of reaction water required to convert the hemihydrate form of plaster to its dihydrate form

a- is less than is required for mixing

b- is greater than the amount required for densite

c- is equal to the amount of water lost by evaporation

d- is equal to the excess water remaining upon setting

2- How does paraffin wax differ from microcrystalline wax?

a- paraffin wax is made from petroleum; microcrystalline wax is not

b- paraffin wax has more volumetric shrinkage upon solidification

c- paraffin wax has a higher melting range than does microcrystalline wax

d- paraffin wax contains polymerized polyethylene molecular chains

3- Which of the following describes the structure of dentin in cross-section near the DEJ compared to dentin near the pulp?

Dentin near the DEJ has…

Diameter		Percent

Tubules/mm2		Of Tubules		Intertubular Dentin

a-	Greater		Larger			Less

b-	Greater		Smaller		More

c-	Fewer			Smaller		More

d- 	Fewer			Larger			More

4- A “smear layer” is caused by which of the following?

a- taking an ireversible hydrocolloid impression

b- investing a wax pattern in gypsum-based investment

c- trimming a densite cast on a model trimmer

d- cutting dentin with a carbide bur

e- etching enamel with an acid gel

5- Dentin that forms prior to eruption of a tooth is called

a- predentin

b- primary dentin

c- secondary dentin

d- reparative dentin

e- intertubular dentin

6- Which of the following expansion mechanisms normally contributes to the total expansion of gypsum-based casting investments, mounting plaster, and densite used for stone dies?

a- hygroscopic

b- thermal

c- setting

d- all of the above

7- Most of the intermolecular bonds that cause irreversible hydrocolloid to set are in molecular regions that are rich in

a- guluronan

b- mannuronan

c- alginic acid

d- phosphate

8- Compared to enamel, dentin has a higher value of which of the following properties?

a- tensile strength

b- hardness

c- elastic modulus

d- compressive strength

e- none of the above

9- When a temporary acrylic bridge is stressed above its proportional limit, which of the following statements must be true?

a- fracture toughness must be exceeded

b- Young’s modulus must be exceeded

c- the temporary bridge will be permanently deformed

d- the temporary bridge will fracture

10- Which of the following two types of hydrocolloid, if any, normally exhibits more permanent deformation upon removal from the mouth after allowing sufficient recovery time ?

a- reversible hydrocolloids

b- irreversible hydrocolloids

c- no difference between the two types, but both exhibit permanent deformation

d- neither exhibits permanent deformation if sufficient recovery time is provided

11- What property is in the denominator of the expression used to calculate Poisson’s ratio for a dental material?

a- percent

b- axial strain

c- Young’s modulus

d- ultimate tensile strength

e- proportional limit

12- Which of the following can be added to paraffin wax to increase the melt range and hardness?

a- carnauba wax

b- beeswax

c- microcrystalline wax

d- cocoa butter

e- Japan wax

13- Consider the following two statements about applying force to a material sample in such a way that the sample returns to its original shape and size when the force is removed:

The stress increases as the applied force is increased.

The strain is inversely proportional to stress

a- both statements are true

b- both statements are false

c- the first statement is true; the second statement is false

d- the first statement is false; the second statement is true

14- Material “A” is more flexible than material “B.”  Which of the following must be true when comparing their stress/strain curves?

a- Material “B” must be tougher than material “A”

b- Material “B” must be more resilient than material “A”

c- Material “B” must have a lower Young’s modulus than material “A”

d- Material “B” must have a higher yield strength than material “A”

e- none of the above

15- Consider the following statement and reason concerning spatulating water and calcium sulfate hemihydrate powder when preparing to pour the mix into a dental impression:

Statement: Within practical limits, excess spatulation shortens the setting time

BECAUSE

Reason: Within practical limits, excess spatulation creates new centers of crystallization

a- Both the statement and the reason are correct and related

b- Both the statement and the reason are correct but not related

c- The statement is correct but the reason is not

d- The statement is not correct but the reason is correct

e- neither the statement or the reason is correct

16- Borax is added to reversible hydrocolloid formulations to improve

a- flexibility

b- elastic recovery

c- setting time

d- strength

e- resistance to imbibitions

17- A difference in fatigue strength between two materials would most directly be due to a difference between the materials regarding of the following properties?

a- yield strength

b- ultimate compressive strength

c- potential for crack propagation

d- hardness

18- Which of the following represents the largest linear dimension?

a- .02 millimeters

b- 2100 micrometers

c- 22,000 nanometers

19- When fully set, irreversible hydrocolloid contains mostly

a- calcium alginate

b- crosslinked mannuronan

c- diatomaceous earth

d- calcium sulfate dihydrate

20- As a group, synthetic waxes used in dental formulations have which of the following properties?

a- Properties for each type are within a narrow range compared to natural waxes

b- Each type is composed of a single molecular species

c- They are synthesized from monomers

d- All of the above

21- Which of the following will be found to a greater extent within an unevenly cooled wax pattern but less so within an evenly cooled wax pattern once the patterns reach the same temperature?

a- flow

b- hysteresis

c- residual stress

d- brittle fracture

22- What is the approximate equivalent of 1 megaPascal in psi?

a- 150 psi

b- 50 psi

c- 15 psi

d- 5 psi

e- .15 psi

23- Complex stresses can be resolved into combinations of which of the following groups of basic stresses?

a- axial and/or compressive

b- axial and/or shear

c- axial and/or bending

d- tensile and/or compressive

e- tensile and/or shear

24- Which of the following entities requires that MSDSs be made available for dental materials?

a- OSHA

b- FDA

c- ADA

d- ANSI

e- ISO

25- The three basic types of dental gypsum are

a- mounting plaster, impression plaster, model plaster

b- model stone, die stone, mounting stone

c- intraoral, extraoral, laboratory

d- hemihydrate, hydrate, dehydrate

e- plaster, hydrocal, densite

26- To increase the compressive strength of gypsum casts, a dentist tries the following:

Chooses hydrocal rather than densite

Increases the amount of mixing water

Adds some “slurry water” to the initial mix

Uses  the cast in a moist state, not dry

How many of these four actions would actually increase the compressive strength?

a- 0

b- 1

c- 2

d- 3

e- 4

27- Compared to most dental materials, dental waxes have relatively high values of

a- compressive strength

b- tensile strength

c- elastic modulus

d- thermal expansion

e- proportional limit

28- Which of the following is an effect of increasing the water-to-powder ratio during the mixing of alginate?

a- decreases setting time

b- decreases strength

c- decreases working time

d- decreases hysteresis

e- decreases surface detail capture

29- The inorganic component of dentin is mostly

a- amelogenin

b- hydroxyapatite

c- collagen

d- rods and prisms

e- phosphophoryn

30- Which of the following categories of information would generally be considered to provide the highest level of evidence to support clinical practice decisions?

a- a systematic review of multiple randomized controlled clinical trials

b- a matched case-controlled clinical study

c- multiple case reports from different institutions

d- reports of clinical simulations using laboratory techniques