NAME (Print):_________________________________________	TUID#:______________________       11/19/07

Instructions: Choose the SINGLE BEST answer.  Circle  a,b,c,d, or e after each question

Microtensile testing is a common way of evaluating which of the following?

- fatigue in denture base resins

- residual stress in wax patterns

- visco-elastic flow of polymeric impression materials

- bond strength of dentin bonding agents

- thermal expansion of gypsum-based casting investment

When compared to human dentin, cold-curing acrylic resin has a higher value of which of the following properties?

- Proportional limit

- Ultimate compressive strength

- Ultimate tensile strength

- Elastic modulus

- None of the above

During polymerization of methyl methacrylate in a chemically-activated system, which of the following is split into two free radicals?

- camphorquinone

- an organic amine

- ethylene glycol dimethacrylate

- methyl methacrylate

- benzoyl peroxide

Which of the following materials has the highest linear coefficient of thermal expansion?

- enamel

- dental amalgam

- resin composite

- inlay wax

- acrylic

What is the function of condensation of dental amalgam?

    - to force the material into all aspects of the cavity preparation

    - to reduce air voids in the final set amalgam

    - to initiate the setting reaction

    - a and b

    - all of the above

Best management practices for managing dental amalgam waste include which of the following:

- disposal of used amalgam capsules by incineration

- use of bleach solution in suction lines to remove residual amalgam

- use of a filter on the suction line and recycling contents of suction line filter

- disposal of non-contact amalgam scrap in biohazardous waste containers

A porcelain crown appears to match adjacent teeth under lighting in the dentist’s office but not in daylight.  This is known as

- anisotropy

- metamerism

- fluorescence

- translucency

- opacity

A polymer exhibits which of the following above its glass transition temperature but not below its glass transition temperature?

- increased ductility

- higher KHN

- less permanent deformation

- brittle fracture

- crystallization

Application of which of the following will increase flow of a thixotropic material, but not of a non-thixotropic material?

- heat

- vibration

- friction

- compressive force

- tensile force

During the setting reaction of high-copper amalgams, “gamma-2” is suppressed by the preferential formation of

  - “gamma-1”

  - “gamma”

  - silver-tin

  - tin-copper

  - silver-copper