- What is the measuring unit for strain?

  - megaPascals

  - grams

  - milliwatts

  - nanometers

  - percent

- Compared to Sample #2, Sample #1 has twice the elastic strain for a given tensile stress.  Therefore, compared to Sample #2, Sample #1 must be

  - weaker.

  - more flexible.

  - less tough.

  - less ductile.

  - harder.

- To demonstrate that a material is ductile, the material must be deformed in excess of its

  - ultimate tensile strength

  - toughness

  - proportional limit

  - Young’s modulus

- A certain dentin bonding agent is reported to have a shear bond strength of 10 megaPascals.  Which of the following is closest to this bond strength in pounds per square inch?

  - 1500 psi

  - 150 psi

  - 15 psi

  - 75 psi

  - 7.5 psi

- Which of the following is equal to a millimeter of dentin thickness?

  - 100 microns

  - 1000 microns

  - 100 nanometers

  - 1000 nanometers

- Which of the following is produced by dehydration under pressure in the presence of water vapor?

  - impression plaster

  - model plaster

  - hydrocal

  - densite

- Which of the following actions will increase the strength of a gypsum cast?

#1- Waiting until the cast has completely dried before using

#2- Using mechanical vacuum-mixing instead of hand spatulation

#3- Increasing water-to-powder ratio

- 1 only

- 1 and 2

- 1, 2, and 3

- 2 and 3

- 1 and 3

- Which of the following, if added to paraffin, would decrease shrinkage during solidification?

  - microcrystalline

  - carnauba

  - barnsdahl

  - montan

- Waxes are generally characterized as having high values of all of the following except one.  Which one is the exception?

  - flow

  - ductility

  - elastic modulus

  - thermal expansion

- Which of the following pairs of materials exhibits the best wetting?

  - amalgam and water

  - acrylic and water

  - Teflon and water

  - etched enamel and occlusal sealants

  - gold casting alloys and dental porcelain

- Intertubular dentin is not normally found in which of the following?

  - primary dentin

  - secondary dentin

  - root dentin

  - peritubular dentin

  - sclerotic dentin

- Which of the following is true regarding dentin and enamel?

  - enamel is anisotropic; dentin is isotropic

  - enamel is isotropic; dentin is anisotropic

  - enamel is anisotropic; dentin is anisotropic (CORRECT)

  - enamel is isotropic; dentin is isotropic (ALSO ACCEPTED, BUT WRONG!)

- Hysteresis is a property of

  - reversible hydrocolloid

  - irreversible hydrocolloid

  - both reversible and irreversible hydrocolloid

  - neither reversible or irreversible hydrocolloid

  - enamel rod structure

- In comparing alginate to reversible hydrocolloid, alginate

  - contains less air

  - captures less detail

  - has greater recovery upon removal

  - contains the same chemical mechanism to retard setting

  - contains the same filler component to provide bulk

- If a manufacturer wants to decrease the setting time of its irreversible hydrocolloid, which of the following changes would be effective?

  - increase calcium alginate proportion

  - increase sodium sulfate proportion

  - decrease sodium sulfate proportion

  - increase sodium phosphate proportion

  - decrease sodium phosphate proportion

- Which of the following color properties should be changed if the dentist wants to make the intensity of the color of a porcelain crown less apparent?

  - fluorescence

  - metamerism

  - hue

  - chroma

  - value (ALSO ACCEPTED BECAUSE “intensity” is somewhat vague)

- To provide the best optical match between an all-porcelain crown and an adjacent natural tooth in the widest range of lighting conditions, both the crown and the natural tooth should exhibit…

  - isomerism

  - metamerism

  - metamerism and fluorescence

  - isomerism and fluorescence

  - fluorescence

- A composite resin surface with numerous 4-micron scratches would be perceived by the patient as

  - dull and rough (A and B accepted: 4um is between “rough and smooth”

  - dull and smooth

  - glossy and rough

  - glossy and smooth

- Based upon thermal diffusivity, which of the following materials would be expected to cause the most thermal shock to a tooth upon application of a hot liquid?

Material		Conductivity	Specific Heat	Density

A		High		Low		Low

B		High		High		Low

C		High		Low		High

D		Low		High		High

E		Low		Low		Low

a-   A

b-   B

c-   C

d-   D

e-   E

- The property that best indicates whether an acrylic base of a new and unused complete denture would fracture upon being dropped and hitting the laboratory tile floor is the material’s…

  - bond strength

  - diametral strength

  - fatigue strength

  - impact strength

- If a material is altered to decrease its KHN, then the material would exhibit greater

  - thermal expansion

  - yield strength

  - resilience

  - resistance to indentation

  - none of the above

- An ideal elastic material with no viscous component has which of the following properties?

  - strain reversal after removal of stress will be time-dependent

  - strain will always be completely reversed

  - strain develops non-linearly upon application of stress

  - strain is independent of modulus

- To perform a useful finite element stress analysis of a dental restoration requires

  - a computer

  - knowledge of the properties of the materials involved

  - samples of the restoration made with the actual materials

  - two of the above

  - a, b, and c

- Compared to conventional amalgams, high-copper dental amalgams exhibit…

  - lower creep

  - lower strength

  - lower marginal integrity in service over time

  - less corrosion resistance in service over time

  - higher amounts of gamma-2 phase

- Which of the following is found in both fully-set conventional and high-copper dental amalgams?

  - gamma-1 phase

  - gamma-2 phase

  - tin-copper phase

  - tin-mercury phase

  - none of the above

- Over-trituration of dental amalgam alloy and mercury causes…

  - decrease in creep

  - decrease in working time

  - decrease in heat generation

  - less gamma-1 formation

  - less gamma-2 formation

- Which of the following best describes the change in the compressive strength of a high-copper dental amalgam occurring from 30 minutes after placement to 24 hours after placement?

  - increases by a factor of 4x or more

  - doubles

  - increases 50%

  - increases 25%

  - increases 10%

- According to best management practices for amalgam waste, which of the following should be placed in biohazard waste receptacles for incineration?

  - non-contact amalgam scrap

  - contact amalgam scrap

  - used amalgam capsules

  - amalgam debris from chairside traps

  - none of the above

- Free radical formation from benzoyl peroxide in dental acrylic polymerization processes is primarily accelerated by which of the following?

  - organic amines

  - light

  - organic amines and light

  - none of the above

- Which of the following is a feature of some condensation-type polymerization systems but not found in addition-type polymerization systems?

  - accelerated by heat

  - water formed as byproduct

  - monomers joined during propagation

  - polymers formed by molecule lengthening

- This methacrylate molecule is at what stage of polymerization?

  - initiation

  - propagation

  - co-polymerization

  - cross-linking

  - termination

- Polymerization of epoxy die material occurs by

  - light activation

  - ring opening

  - hydrosilyation

  - condensation

- Which of the following is/are removed from dentin by the total etch procedure?

  - hybrid zone

  - enamel rods

  - smear plugs

  - odontoblasts

  - none of the above

- Which of the following is a hydrophilic primer coupling agent commonly found in current dentin bonding systems?

  - PMMA

  - HEMA

  - Bis-GMA

  - UDMA

  - MMA

35- Which of the following is not a feature of the bonding system category abbreviated: [EP]+B  ?

a-    provides for bonding to both dentin and enamel

b-    requires rinsing enamel and dentin after etching

c-    creates a hybrid zone in dentin when completed

d-    is delivered to the dentist as a two-bottle system

  - What is the approximate thickness of hybrid zones in dentin created by current bonding systems?

- 1 millimeter

- 0.1 millimeters

- 1 nanometer

- 300 microns

- 3 microns

  - In the current bonding systems using a 37% phosphoric acid gel etch and water rinsing, which of the following is true regarding the smear layer and smear plugs after water rinsing?

- they will collapse if air-dried

- they will both become infiltrated with hydrophilic resin(s)

- only the smear plugs will become infiltrated with hydrophilic resins

- only the smear layer will become infiltrated with hydrophilic resins

- none of the above

  - Camphorquinone is found in which of the following types of composite resins?

- visible light-cured and dual-cured

- visible light-cured and self-cured

- visible light-cured

- self-cured

- dual-cured

  - If a manufacturer failed to use silane in the production of a direct universal hybrid composite resin, what would be the expected effect of this error?

- increase in modulus

- increase in hardness

- increase in translucency

- increase in crack propagation

- increase in polymerization shrinkage

  - In an uncured composite resin, where is TEGMA found and what effect does it have when present?

Location			Effect

a-	continuous phase		binds filler

b-	continuous phase		decreases viscosity

c-	continuous phase		decreases shrinkage

d-	dispersed phase		binds filler

e- 	dispersed phase		forms hybrid layer

  - The “C-Factor” in a composite resin restoration refers to the…

- ratio of bonded to unbonded surfaces

- volume percent polymerization shrinkage

- ratio of bonded enamel area to bonded dentin area

- volume percent of restoration consisting of filler particles

  - For which of the following would a gypsum-based casting investment not be appropriate?

- gold alloy onlay

- full gold alloy crown

- porcelain/metal crown undercasting

- cast post and core under a porcelain/metal crown

- all of the above can be cast using a gypsum-based casting investment

  - What is the approximate total percent expansion required from all sources within a gypsum-based casting investment?

- none

- 0.015%

- 0.15%

- 1.5%

- 15%

  - A cast gold alloy crown has rounded margins instead of the sharp margins that were produced in the wax pattern.  Which of the following actions could correct this problem upon recasting?

- place pattern more than 8mm from mold top / end

- increase centrifugal casting force

- decrease sprue diameter

- two of the above

- a, b, and c, above

  - What is the optimum region of application of the air/gas torch flame to melt alloy ingots for centrifugal casting?

- in the center of the orange zone

- at the tip of the orange zone

- in the center of the oxidizing zone

- at the tip of the oxidizing zone

- at the tip of the reducing zone