- Material Safety Data Sheets (MSDSs) for dental materials are required by the FDA.

  - True

  - False

- Restorations made on a gypsum die are called “direct” restorations.

  - True

  - False

- The temporomandibular joint represents the fulcrum in the masticatory system.

  - True

  - False

- Poisson’s ratio is the ratio of a sample’s (axial length while under axial tension or compression) to (original axial length).

  - True

  - False

- On a stress/strain curve of a ductile material, there is always permanent deformation of the sample for applied stresses that are above the proportional limit of the material.

  - True

  - False

- Thermal expansion normally occurs during the setting reaction of dental stone used for fabricating study casts.

  - True

  - False

- Roughening the surface of a sample would increase the total surface energy of the surface as a system.

  - True

  - False

- Substituting “slurry water” for tap water when mixing dental stone powder and water will decrease setting time of the mix.

  - True

  - False

- Irreversible hydrocolloid exhibits syneresis during gelling.

  - True (due to possible confusion in reading assignment)

  - False

- Alginate sets by the formation of intermolecular bonds that include sodium.

  - True

  - False

- When added to paraffin, carnauba wax decreases the hardness of the solid wax.

  - True

  - False

- Dental waxes are generally characterized as having high ductility and low thermal expansion.

  - True

  - False

- Dissolution of enamel will normally occur at a pH greater than 5.5.

  - True

  - False

- A millimeter is equal to 1000 microns.

  - True

  - False

- Stress is proportional to force and inversely proportional to area.

  - True

  - False

- Permanent deformation occurs in both reversible and irreversible hydrocolloid impression materials upon setting and removal from undercut areas in the mouth .

  - True

  - False

- Force is measured in megaPascals or Pascals.

  - True

  - False

- If a sample of metal orthodontic wire is stressed to its 0.2% yield strength, which of the following statements must be true?

  - the fracture toughness of the wire has been slightly exceeded

  - the metal is not ductile

  - the wire was not stressed above its proportional limit

  - the ultimate tensile strength of the wire has been exceeded

  - the wire has been permanently deformed

- A material with low fracture toughness will always exhibit which of the following properties compared to one with a high value?

  - less able to be formed into a sheet

  - less able to be formed into a wire

  - higher Poisson’s ratio

  - less able to resist crack propagation

  - lower Young’s Modulus

Strain

Stress

D

A

B

C

- Referring to the diagram above, which material had no permanent deformation?

  - A

  - B

  - C

  - D

  - None

- Which of the following is added to reversible hydrocolloid to improve the strength of the set hydrocolloid?

  - diatomaceous earth

  - potassium sulfate

  - water

  - borax

- The “memory effect” of dental inlay pattern waxes is primarily caused by

  - low thermal expansion of inlay pattern wax

  - residual stress in the wax pattern

  - burning of the wax during the wax-up process

  - volatilization of some wax components

  - presence of microcrystalline wax

- Dentin that forms in response to localized tooth wear is called

  - mantle dentin

  - primary dentin

  - peritubular dentin

  - intertubular dentin

  - tertiary dentin

- The inorganic component of enamel is mostly

  - amelogenin

  - hydroxyapatite

  - collagen

  - non-collagenous proteins

  - phosphophoryn

- Compared to enamel, dentin has a higher value of which of the following?

  - hardness

  - Young’s modulus

  - tensile strength

  - (a) and (b)

  - none of the above

- The stone powder as purchased from a dental materials supplier that is used to make a dental study cast is mostly composed of

  - calcium sulphate hemihydrate

  - calcium sulphate dehydrate

  - potassium sulfate

  - gypsum

- Which of the following requires the least amount of mixing water to obtain the same consistency of mix, assuming equal weights of each powder?

  - densite

  - plaster

  - hydrocal

  - none, they all require the same amount of mixing water

- To increase the compressive strength of her patient’s gypsum cast, a dentist tries the following:

Chooses hydrocal rather than densite

Increases water-to-powder ratio

Delays use until the cast is fully dried

How many of these actions would actually increase compressive strength?

- 0

- 1

- 2

- 3

- 4

- Dehydration of gypsum under pressure in the presence of water vapor creates hydrocal.

  - True

  - False

- Which of the following describes the structure of dentin in cross-section near the pulp chamber compared to near the DEJ?

Dentin near the pulp chamber has…

Diameter 	Percent

Tubules/mm2 	Of Tubules	Interbular Dentin

- Fewer		Smaller	More

- Fewer		Smaller	Less

- Fewer		Larger		More

- Greater	Larger		Less

- Greater		Smaller	More

- For the purpose of retarding the setting reaction, regular set alginate powder has more of which of the following compounds compared to fast set alginate powder?

  - Sodium phosphate

  - Calcium sulphate

  - Guluronan

  - Calcium alginate

  - None of the above

- What is the effect of decreasing the water/powder ratio on the following properties of  irreversible hydrocolloid?

  - increases working time

  - increases strength

  - increases setting time

  - increases syneresis

- Consider these statements about synthetic waxes used in making dental waxes:

Synthetic waxes typically have narrow-range physical and mechanical properties

BECAUSE

Synthetic waxes are synthesized from monomers resulting in a single species

- Both the statement and the reason are correct.

- The statement is correct but the reason is not.

- The statement is not correct, but the reason is correct.

- Neither the statement nor the reason is correct.