1- Which of the following information sources for evidence-based practice is the most reliable for selecting a dental material?

- animal studies involving dental materials

- laboratory studies of materials properties

- long-term clinical trials of materials

- deductions from clinical literature on dental materials

2- Which of the following restorations is an “indirect” restoration?

- Occlusal sealant

- Amalgam restoration

- Composite resin restoration

- Cast gold crown

- Ionomer restoration

3- Consider the following two statements:

The stress increases as the applied force is increased.

The stress is inversely proportional to the area over which the force is applied.

- Both statements are TRUE.

- Both statements are FALSE.

- The first statement is TRUE, the second statement is FALSE.

- The first statement is FALSE, the second statement is TRUE.

4- An axial tensile stress is applied to a 40.0 mm rod of dental acrylic resulting in an elongation to 40.8 mm.  What amount of strain has occurred?

- none

- 0.2%

- 1.0%

- 2.0%

- 0.8mm

5- Consider two different dental materials, each with the same amount of toughness.  Which of the following statements describes a correct relationship of various properties for the two materials?

- The modulus of elasticity MUST be the same.

- The ductility MUST be the same.

- The ultimate tensile strength MUST be the same.

- The proportional limit MAY be the same.

Strain

Stress

A

D

C

B

Refer to the stress-strain graph of four materials (A, B, C, D), above to answer the next three questions:

6- Which material is the least ductile?

- A

- B

- C

- D

7- Which material is the stiffest?

- A

- B

- C

- D

8- Which material has the lowest ultimate tensile strength?

- A

- B

- C

- D

9- If a substance is added to a dental material to decrease its KHN, resistance to which of the following will be DECREASED by definition?

- crack propagation

- surface absorption of light

- indentation

- fracture

- flow

10- The rate at which a body with non-uniform temperature approaches equilibrium is

- inversely proportional to the conductivity of the material.

- inversely proportional to the density of the material

- independent of the density of the material.

- independent of the specific heat of the material.

11- In examining the surface of a metallic dental restoration that has functioned intra-orally for several years, you notice that the surface is pitted with visible loss of material.  This condition is most likely due to which of the following?

- resistivity

- galvanism

- tarnishing

- corrosion

- percolation

12- Which of the following color properties should be INCREASED if the dentist wants to make the intensity of the color of a porcelain crown more apparent?

- hue

- chroma

- value

- fluorescence

- metamersim

13- Consider the following two statements concerning dental plaster and dental stone:

Dental stone is stronger than dental plaster.

BECAUSE

Dental stone is produced by the process of “wet calcination”.

- Both the statement and the reason are correct and related.

- Both the statement and the reason are correct but not related.

- The statement is correct but the reason is not.

- The statement is not correct, but the reason is correct.

- Neither the statement nor the reason is correct.

14- You are pouring a dental stone cast and want to decrease the setting time of the mix so that you can use the cast sooner.  How can you accomplish this?

- use “slurry water”

- if using mechanical mixing, add vacuum

- use colder water

- mix die stone with model stone in 50:50 ratio by weight

15- In creating a gypsum cast, a dentist does the following:

Chooses stone rather than plaster

Uses hand spatulation rather than mechanical vacuum-mixing

Waits until the cast has fully dried after setting rather than using it immediately

Which of the following statements is true regarding these three actions?

- All three actions are effective in increasing the strength of the  cast as used.

- Only one action will decrease the strength of the cast as used.

- One action is irrelevant to the strength of the cast as used.

- Only one action is effective in increasing the strength of the cast as used.

16- Which of the following expansion mechanisms contributes to the overall expansion of gypsum-based casting investments, but not to expansion of gypsum used for producing stone study casts?

- setting

- thermal

- polymeric

- hygroscopic

17- Borax is added to reversible hydrocolloid formulations to improve

- gelling time.

- hysteresis.

- strength.

- flexibility.

- syneresis.

18- Exudation of water accompanied by shrinkage of reversible hydrocolloid is called

- metamerism.

- imbibition.

- syneresis.

- viscoelasticity.

- hysteresis.

19- Which of the following reacts with mixed unset alginate to form irreversibly set alginate?

- sodium phosphate

- calcium phosphate

- sodium sulfate

- calcium sulfate

20- A 4.5% permanent set is typical of

- reversible hydrocolloids but not irreversible hydrocolloids

- irreversible hydrocolloids but not reversible hydrocolloids

- neither irreversible hydrocolloids nor reversible hydrocolloids

- both irreversible hydrocolloids and reversible hydrocolloids

21- Alginate sets by the formation of intermolecular bonds involving

- sodium.

- phosphate.

- fluoride.

- calcium.

- sulfate.

22- All of the following are ways to minimize distortion in castings related to wax patterns except one.  Which one is the EXCEPTION?

- Heat wax uniformily to 1000C for 15 minutes prior to making the pattern.

- After making the wax pattern, invest it without delay.

- Store the wax pattern at a low temperature if not invested right away.

- Completely burn out the wax pattern so that no wax residue remains.

23- Carnauba wax can be added to paraffin to provide which of the following pairs of properties of the final blend compared to paraffin alone?

- decrease melt range and increase tackiness

- increase melt range and increase hardness

- decrease tackiness and decrease hardness

- increase heat retention and increase thermal expansion

- decrease heat retention and decrease hardness

24- Which of the following is an example of a thermoset polymer?

- polystyrene

- PMMA

- cross-linked poly(methyl methacrylate)

- all of the above

25- Which of the following would a material exhibit ABOVE its glass transition temperature compared to that BELOW its glass transition temperature?

- increased ductility

- higher KHN

- less permanent deformation

- brittle fracture

26- During polymerization of poly (methyl methacrylate) in a light-activated system, which of the following is split to form two free radicals?

- camphorquinone

- an organic amine

- ethylene glycol dimethacrylate

- benzoyl peroxide

27- Which the following clinical stage descriptions for the polymerization of powder/liquid cold-cured poly (methyl methacrylate) is the THIRD stage?

- dough-like

- runny

- sandy

- hard

- rubbery

28- Which of the following polymers are formed by addition polymerization?

- PMMA

- bis-GMA

- both PMMA and bis-GMA

- neither PMMA nor bis-GMA

29- When compared to human dentin, polymerized acrylic resin has a higher value of which of the following properties?

- Proportional limit

- Ultimate compressive strength

- Ultimate tensile strength

- Elastic modulus

- None of the above

30- Triad™ resin has which of the following features?

- Cured form is PMMA

- Light activation via camphorquinone

- Lack of oxygen-inhibited surface layer

- Unfilled

- Lack of polymerization shrinkage